## Slide 1: SRF Development for CW Ion Linacs
Sang-hoon Kim SRF Systems Engineering and Testing Group Leader

## Slide 2: High-performance CW Medium-β Elliptical Cavity Cryomodule For Next-generation CW Ion Linacs such as the FRIB Energy Upgrade (FRIB400)
Importance
  FRIB400 is a CW linac, so higher Q0 and better field-emission (FE) performance are required compared to pulsed linacs such as SNS and ESS
  Successful development of a high-performance cavity and high-power fundamental power coupler (FPC) will allow FRIB400 to be cost-effective and reliable
Challenges
  High Q0 recipes were extensively studied for the 1.3 GHz TeSLA cavity (nitrogen doping, medium-temperature baking, …), but not for 644 MHz
  Need to develop a new high-power FPC for 15 kW CW at 644 MHz
  Resonance-control stability is needed against microphonics and ponderomotive instabilities due to higher QL compared to pulsed linacs
  Lack of US vendors for SRF cavity production
Accomplishments
  MSU/ANL/FNAL achieved state-of-the-art performance with medium-β multi-cell Nb cavities with EP and N-doping (first demonstration in this cavity class)
Path forward
  High Q0 R&D: flux expulsion in cryomodules, recipe optimization for 644 MHz, EP optimization for high-aspect-ratio medium-β cavities
  Develop FE-free methods and techniques
  Develop FPC and demonstrate stable resonance control;validate in a cryomodule test
  Upgrade the FRIB SRF Facility: EP, N-doping
Need strong support for this R&D, similar to 1.3 GHz TESLA cavities (latter supported by HEP and BES)
Cavity | Specification/ Design Goal
FRIB400: βopt = 0.65 644 MHz 5-cell; CW | D: 2x1010 @ 17.5 MV/m, 2.0 K (under development)
SNS β = 0.61 805 MHz 6-cell; pulsed | S: 5x109 @ 10.2 MV/m, 2.1 K (operational since 2007)
ESS β = 0.67 704 MHz 6-cell; pulsed | S: 5x109 @ 16.7 MV/m, 2.0 K (under construction)
PIP-II LB650: βG= 0.61 650 MHz 5-cell; CW | S: 2.3x1010 @ 16.9 MV/m, 2.0 K (under development*)
*as of June 2021 (SRF2021)
FRIB400 Design goal
FRIB400 R&D cavities

## Slide 3: Plasma Processing for Low-β Coaxial Cavities To Achieve High Availability in Long-term Operation of SC ion Linacs such as FRIB
Importance
  In long-term operation, particularly with high-intensity heavy-ion beams, SC cryomodules may suffer from increased FE, which could eventually reduce the beam energy
  In-situ plasma processing is useful to recover performance with little adverse impact on schedule and budget, as shown at SNS
Challenges
  Avoid coupler breakdown in spite of higher Qext and absence of higher-order model (HOM) couplers for CW linacs compared to pulsed linacs
  Develop effective plasma cleaning for coaxial cavity shapes: no extensive studies so far compared to elliptical cavities
Accomplishments
  Preliminary studies: achieved FE reduction with plasma processing for 2 out of 3 FRIB β = 0.085 QWRs with FPCs using the 5λ/4 HOM
Path forward
  More statistics one plasma processing with vertical tests
  Demonstrate plasma processing in cryomodules with offline tests
  R&D to better understand plasma processing:
    Simulations, e.g. plasma density with HOMs
    Diagnostics, e.g. measure the plasma potential (concern: Cu sputtering at coupler), plasma density with HOMs
So far, plasma processing development work for low-β coaxial cavities is a small-scale effort under the auspices of FRIB Operations
Ne-O plasma
Field emission reduction with plasma processing
Plasma processing setup: FRIB β = 0.085 QWR with FPC

## Slide 4: Pushing the Performance Limits of Low-β Coaxial Cavities Transformative Surface Preparation for FRIB β=0.53 HWRs
Importance
  While the FRIB linac cavities meet the gradient requirements (Ea = 7.4 MV/m for β = 0.53 HWRs), higher fields (e.g. Ea = 10 MV/m), would provide additional science opportunities: higher beam energy and/or improved reliability against cavity failures
Challenges
  High-field Q slope (HFQS) appears at Ea ~ 9 MV/m (Bp ~ 80 mT) and hampers reliable operation at Ea = 10 MV/m within the FRIB cryo budget
Accomplishments
  Preliminary studies: EP + in-situ 120⁰C baking (ILC recipe) shows promising results for reducing HFQS
Path forward
  More statistics on EP + baking with vertical tests
  Study of other recipes, e.g.
    ‘Wet’ doping without heat treatment
    Furnace low- to medium-temperature baking
An R&D project is now funded by DOE-NP: “Development of transformative preparation methods to push up high Q&G performance of FRIB spare HWR cryomodule cavities” (PI: K. Saito, MSU; September 2022 - August 2024)
EP on β = 0.53 HWR at FRIB
Performance improvement with
EP + in-situ baking

## Slide 5: Concluding Remarks
More support is needed for R&D on low- and medium-β SRF cavities. Underfunded areas include
  High Q0 R&D for medium-β elliptical cavities
  Plasma processing R&D for low-β coaxial cavities
Continuing support for low-β SRF technology development is necessary for world leadership amongst the SRF community
Continued technology development in these areas will facilitate reliable operation of existing machines and cost-effective construction of new machines for NP as well as HEP, BES, and industrial applications